DESCRIPTION

PLASTiFLO acts as a cement and colour dispersion agent in the render wet mix as well as a water reducer. PLASTiFLO acts as non-aerating plasticizer.

The work effort necessary applying the wet render to brickwork is far less than conventional cement sand mixes. It is quite noticeable there is less strain on the elbows and shoulder joints.

APPLICATIONS

PLASTiFLO is used as an additive for renders, floats, and mortars.

BENEFITS

- Decreases work effort when wet mix applied.

- Improved aesthetics, brighter, even colours.

- Improved structural integrity of products, better strength, and abrasion resistance.

- One product for colourant and cement dispersion.

- Minimal cost per mix.

- Has the ability to slightly reduce cement in mixes whilst increasing strength and abrasion of finished products.

- Render/floats can be skim plastered with TITAN One Bag Hardwall plaster finish after one day on a suitably prepared render/float. Lime/plaster can be applied to the floats etc. as normal.

PRODUCT USAGE

SAND CEMENT FINISH RENDER/FLOATS

EXTERNAL OR INTERNAL

As a guide, 40 millitres(mls) of PLASTiFLO is added per 20kg bag cement based on a 1:4 to 1:6 cement/sand render. Half the normal water should be added to the mix prior to adding PLASTiFLO. Let mix, then add water to achieve the desired slump or consistency.

BRICKLAYING

As a guide 40 mls of PLASTiFLO is added per 20kg of GP cement based on mixes from 1:4 to 1:6 cement: sand respectively. Half the normal water should be added to the mix prior to adding PLASTiFLO. Let mix, then add water to achieve the desired slump or consistency.

If hydrated lime powder is added, only add an eighth of a shovel per mix. Hydrated lime addition is not considered necessary when using PLASTiFLO in the mix.

STORAGE

Store PLASTiFLO in sealed containers under cover in a cool area away from foodstuffs.

CLEAN UP

Clean up PLASTiFLO with absorbent material and dispose of according to state and federal laws.

PACK SIZES

PLASTiFLO is sold in packs of 5 and 20 litres.

TRANSPORT

PLASTiFLO is not a hazardous or dangerous product for transport under the guidelines of Safe Work Australia.