DESCRIPTION

TITAN SKIM PLASTER is formulated to use as a thin veneer leveling finish on TITAN HARDWALL where there are slight undulations in the finish. The same product can be used general internal patching.

The finished in place set TITAN SKIM can be sanded with fine sandpaper if necessary and painted after being sealed.

MIXING

For 100mls of water, add in the region of 150ml (200g) of TITAN SKIM to the water and allow a few minutes for it to soak into the water. Mix it thoroughly with a spatula until smooth and creamy.

Apply the mix to a dry wall with a wide spatula or small plasterer’s trowel as a thin veneer filling medium.  If tearing occurs, which can occur on very dry substrates, spray a little water mist onto the skimmed area and trowel off.

COVERAGE

Coverage of 1kg of TITAN SKIM PLASTER mixed with water is approximately 1.5m2 as a veneer application.

CLEAN UP

In the wet state, clean up is done with water.

STORAGE

Store all products under cover in a cool area away from foodstuffs. Keep the products sealed when not in use or after each use.

SAFETY

Wear coverall, safety boots and glasses respectively. Gloves are optional to wear but recommended.

PACK SIZES

TITAN is sold in packs of 1kg and 5kgs.

TRANSPORT

TITAN is not a hazardous or dangerous good as defined by Safe Work Australia.